POLYMERS  (3 MARKS)

SECTION A

Elastomers: Rubber like solids which can be stretched due to presence of weakest intermolecular forces between polymeric chain and which retract to their original position due to presence of few cross links between the chains.

Ex. Vulcanised rubber.

Fibre: Polymers which possess high tensile strength and high modulus due to strong intermolecular forces like H – bonding and which  have crystalline nature,close packing of chains,sharp M.P.are called as fibres. These are used as fibres.

Ex. Nylon 6,6.

Difference between thermo plastics and thermosetting polymers.

|  | Thermo plastics |  | Thermosetting polymers |
| --- | --- | --- | --- |
| 1 | inter molecular force between polymeric chains are intermediate between weak van der Waal’s force and H- bond and there is no cross linkingdue to extensive cross linking | 1 | Extensive cross linking between polymeric chains and therefore intermolecular force is stronger than thermoplastic |
| 2 | Easily moulded to a desired shape by heating | 2 | Become infusible and form an insoluble hard mass on heating |
| 3 | contains linear or slightly branched long chain molecules | 3 | contains cross linked or heavily branched long chain molecules molecules |

Synthesis of ethene:

n CH2 = CH2    polymerisation         [-CH2 -   CH2- ]-  n

Ethene                                               Polythene

Synthesis of LDP:

n CH2 = CH2    polymerisation

Ethene                                                LDP

1000 -2000atm.

traces of O2 or peroxide

Synthesis of HDP:

n CH2 = CH2    polymerisation

HDP

Ethene

333 to 343K ,6-7 atm.

Benzene or toluene solvent

Zieglar  - Natta catalyst

Synthesis of Teflon:

Persulphate catalyst

n CF2 = CF2 	-(-CF2  -  CF2-) -n

high pressure

Synthesis of polyacrylonitrile:

CN

polymerisation		  CN

n CH2 = CH	  -(-CH2  - CH-)-n

Peroxide catalyst

Synthesis of Nylon – 6,6:

O               O

║                 ║

H –O – C – (CH2)8- C –O – H   +   H2N – (CH2)6 – NH2

Adipic acid (1,10- Decanedioic acid )       Hexamethylene diamine

553K     High pressure

Nylon- 6,6.

Synthesis of Bakelite:                          OH                   OH                 OH

CH2OH     CH2OH          CH2OH                                                                                    CH2OH

H+ or OH-	+	+

CH2OH	CH2OH	CH2OH

OH	OH	OH	    OH

CH2OH                                                         Heated with HCHO                                                  Novolac

OH                       OH                    OH

H2C	CH2	CH2	CH2

CH2                   CH2                    CH2

H2C	CH2	   CH2	CH2

OH                    OH                     OH   Bakelite

Resin intermediate

Melamine

NH – CH2 -)-

- (- HN

polymerization

NH

Melamine  formaldehyde

Synthesis of PHBV:

OH	     OH

CH2 – CH – CH2 – COOH + CH3 –CH2 – CH – CH2 – COOH

-(-O –CH—CH2-C –O – CH – CH2 –C -)-n

║                              ║

CH3	      O	        CH2CH3       O

PHBV

Uses of different polymers

- Polyppropene : manufacturing of ropes,toys,pipes fibres.

- Polystyrene: as an insulator,as a wrapping material,manufacturing of toys,radio and television cabinets

- PVC : to make rain coats,hand bags,in vinyl flooring , water pipes.

- urea formaldehyde resin :to make unbreakable cupd and laminated sheets

- Glyptal/Terylene/Dacron: to make paints and lacquers

- Bakelite: to make combs,electrical switches,handles of utensils,computer discsLDP: insulation of electricity carrying wires,manufacture of squeeze bottles,toys and flexible pipes.

- HDP: to make buckets,dustbins,bottles,pipes .

- Draw structures for natural rubber and vulcanized rubber.

H3C	       H

H3C 	H	CH2	CH2	C = C

C = C 	CH2

----H2C	CH2	=                                                 CH2---

H3C                    H

Natural rubber (cis-polyisoprene)

CH3	        CH3

-----CH2 – C –    CH – CH2 ----     ----CH – C = CH –CH2 ----

S        S                            S

-----CH2 – C –    CH – CH2 ----     ----CH – C = CH –CH2 ----

CH3                                  CH3

vulcanised rubber

SECTION B

1. What are polymers?

2. How are polymers classified on the basis of structure?

On the basis of structure polymers are classified into three classes

(i) Linear polymers: Polymers containing long  straight polymer chains .

Ex.  High density Polythene, PVC.

(ii) Branched chain polymers: Linear polymer chains having some branches

Ex.  Low density polythene

(iii) Cross linked or network polymers: Polymers containing strong covalent

bonds

between various linear polymer chains  and which are formed from

bi-functional

and tri-functional monomers.

Ex. Bakelite, melamine formaldehyde.

3. Write the names of monomers of the following  polymers.

(i)

O                 H

║                    │

(ii)     ─ C – (CH2)5 – N ─        (iii)  ── CF2  ── CF2

n

n

(i)   Hexamethylene diamine  or Hexane -1.6- diamine. and Hexane –1,6 -

dioic acid.

(ii)   6 – aminohexanoic acid

(iii)  Tetrafluoroethene

4. Classify the following as addition and condensation polymers.

Terylene,Bakelite,

Polyvinyl chloride,Polythene.

Addition polymers: Polyvinyl chloride, Polythene

Condensation polymers: Terylene, Bakelite

5. Explain the difference between Buna – N and Buna – S

Buna – N is a co-polymer of 1,3 – Butadiene and Acrylonitrile

Synthesis of Buna –N:

CN                                                                CN

n CH2 = CH – CH = CH2 + n CH2 = CH                       ( -CH2 - CH = CH - CH2 – CH2 –CH )n

1,3 –Butadiene.              Buna – N (Butadiene acrylonitrile co-polymer)

Buna – S is a co-polymer of 1,3 – Butadiene and styrene.

For Buna – N (Refer below)

6. Arrange the following polymers in an increasing order of their intermolecular forces.

(i)  Nylon- 6,6, Buna – S , Polythene

(ii) Nylon- 6 , Neoprene, Polyvinyl chloride.

- Buna - S,Polythene, Nylon- 6,6

- Neoprene, Polyvinyl chloride ,Nylon- 6

7. Is       [-CH2 – CH (C6H5) -] n  a homopolymer or a co-polymer?

It is a homopolymer and the monomer form which it is obtained is

C6H5 – CH = CH2

8.What are polyesters ? Give an example. Give an example for

a biodegradable poly ester.

9.Polymers synthesized by the condensation   of  dicarboxylic acids

and diols.

Ex. Terylene

Ex. For a biodegradable poly ester is PHBV

i.e.Poly β- hydroxyl  butyrate- co- β-hydroxyl valerate

SECTION C

CBSE 2008

1.Define the term polymerization. (1)

The process of formation of macrosized molecules of high molecular mass

in which very large number of repeating structural units are joined together

by covalent bonds.

2.Distinguish between homopolymers and co- polymers  (2)

Homopolymers                                               co- polymers

1. Polymers made by

polymerization                                      1.Polymers made by addition

of a single type of monomer	                 polymerization or condensation

polymerization of two or more

different types of monomers

2. contains multiple units of                      2. contains multiple units of

the same single  monomer                                        two different monomers.

Ex. Polythene,Nylon-6.                                            Ex. Buna – S,Nylon-6,6

CBSE 2007

1.Write formulae of monomers of polythene and Teflon.  (2)

Monomer of polythene   CH2 = CH2

Monomer of Teflon        CF2  =  CF2

- Write the structures of monomers used and  one use of each of

the following         polymers. (a) Teflon (b) Buna – N    (2)

OR

What are biodegradable polymers ? Give two examples.   (2)

Teflon is used to make non – stick surface coated utensils.

Monomers  of Buna -  N (i)  CH2 = CH – CH = CH2 1,3 –Butadiene.

CN

│

(ii) CH2 = CH   Acrylonitrile.

Buna -  N is used to make oil seals and tank linings.

OR

Biodegradable synthetic polymers containing functional group similar to the functional groups present in biopolymers and which are made to avoid  environmental problems made by polymeric solid wastes.

Ex. 1. Poly β-hydroxybutyrate –co- β –hydroxy valerate (PHBV)(2) Nylon-2-nylon-6.

CBSE 2005

What are biodegradable polymers . Write the structural formula of a biodegradable polymer.   (2)

H              O   H                   O

│                ║     │                      ║         Nylon-2 nylon-6

-  ─ N -  CH2 – C – N –   (CH2) 5     C-  ─

n

CBSE 2004

Write the mode of free radical addition polymerization of an alkene. Clearly indicate the role of an initiator in it.   (2)

Mixture of ethene and benzoyl peroxide is exposed to sun light or heated.

Formation of free radical:

O                             O                                                     O

║     . .        . .          ║                                                     ║                          .

C6H5 – C  - O ──   O  -     C – C6H5                                 2C6H5 –  C   –  O.  :  + 2 C6H5

. .      . .                                                             ..

Phenyl radical

Benzoyl peroxide

Chain initiation step:

.                                                        .

C6H5   +  CH2 = CH2                                 C6H5  - CH2  - CH2

Chain propogation step:

.                                                                                         .

C6H5  - CH2  - CH2    +  CH2 = CH2                          C6H5  - CH2  - CH2   -  CH2  -  CH2

nCH2 = CH2                          		.

C6H5  ( CH2  - CH2   )    n   - CH2  -  CH2

Chain terminating step :

.

C6H5  ( CH2  - CH2   )n   - CH2  -  CH2

.

C6H5  ( CH2  - CH2   ) n   - CH2  -  CH2

C6H5  ( CH2  - CH2   ) n   - CH2  -  CH2  ─ CH2  -  CH2 – (CH2  -  CH2)n –C6H5

Polythene

Write equations for synthesis of following   (i) Glyptal  (ii) Neoprene  (2)

- Glyptal:

O                  O

║	                     ║

n H- O -H2C – CH2  - O- H  + n  H – O – C                C – O – H

Ethylene glycol                                                    Pthalic acid

(Ethane -1,2 –diol)                                                   (1,4 – Benzene – dicarboxylic

acid)

- nH2O

O                 O

║                ║

-( O -H2C – CH2  -  O-  O – C               C – ) n

Glyptal/Terylene/Dacron

- Neoprene

Cl

Cl                                                                   │

│                         Polymerisation   (- CH2 - C  = CH - CH2 -)n

n CH2 = C  - CH = CH2

2 – Chloro – 1,3 – butadiene                            Neoprene

CBSE  2003

Write equations used for synthesis  of (i) Terylene (ii) Neoprene  (2)

Write equations for synthesis of (i) Nylon – 6 (ii) Buna –S   (2)

(i) Nylon- 6 :

Caprolactum

O                 H

║                     │                  Nylon - 6

- C –( CH2 )5 – N -

n

(ii) Buna  - S: 	 C6H5

│

nCH2 = CH – CH = CH2   + n CH 2 =  CH

1,3 –Butadiene.                 Styrene (Phenylethene)

C6H5

│

(  - CH2  - CH = CH  - CH2  - CH2  - CH  -)

Butadiene styrene copolymer(Buna –S)

CBSE 2002

Write names and structures of monomers of following polymers.   (i) natural rubber  (ii) Terylene       (2 marks)

- Natural rubber:

CH3

│

CH2 = C  - CH = CH2  isoprene(2 – Methyl -1,3 – butadiene)

Write the information asked for the following polymers

- Bakelite: materials used for its preparation

- Synthetic rubber – monomer unit.  (iii) PVC ; monomer unit.  (iv) Nylon -66 materials required for preparation.  (2)

- Bakelite: Phenol and formaldehyde

- Synthetic rubber: monomer is  Chlorpprene .,

Cl

│

Monomeric unit is(- CH2 - C  = CH - CH2 -)

Cl

│

- PVC : monomer Vinyl chloride, Monomeric unit is (- CH2 – CH - )

(iv)     Nylon – 6,6: (1) Hexamethylenediamine (2) Adipic acid

Explain the following terms with suitable examples in each case(i) chain growth polymerization (ii) step growth polymerization.  (2)

- chain growth polymerization :

The process of formation of polymer by simple addition of molecules of the same or different unsaturated monomers is called as chain growth polymerization or addition polymerization.

Ex. Synthesis of polythene (Refer above)

- Step growth polymerization: The process of formation of polymer by repeaeted condensation reaction between two bi –functional monmers is called step growth polymerization or condensation polymerization

Ex. Synthesis of Terylene (Refer above) .

CBSE 2001

Write names and strctures of the monomers of each of the following polymers. (i) Natural rubber (ii) Buna –S    (2)

CBSE 1999

How are Buna – S and Terylene synthesized? Give chemical equations .  (2)

CBSE 1996

Mention which of the following are addition polymers ? (i) Terylene (ii) Nylon -66  (iii) Neoprene (iv) Teflon  (2)

SECTION -  D  (Higher order questions for high achievers)

- What do you mean by chain transfer agent?

The reagent that react with the growing chain in addition polymerization to interrupt the further growth of original chain and in which product of such a reaction will initiate its own chain growth  to form a new polymer with lower molecular mass.

- What is an inhibitor in polymerization ? Give an examole. The highly unreactive radical formed by chain transfer agent if if inhibit further polymerization and leads to chain termination is called as inhibitor.Ex. Benzoquinone.

- What is addition polymerization? Explain the mechanism of addition polymerization. (Vinyl polymerization)      .

Chain initiating step:   In – In                    2 In  (initiator)

.                                                        .

In  +    CH2 = CH                In - CH2 - CH

│                                        │

G                                  G

Chain propagating step:

.                                                                   .

In - CH2 - CH   +   CH2 = CH                    In - CH2 - CH  - CH2 - CH

│                        │                                  │                  │

G                      G                            G                G

n  CH2 = CH

│

G

.

In –( CH2 - CH - ) n- CH2 - CH

│	         │

G	       G

Chain terminating step:

.                      .

In –( CH2 - CH - ) n- CH2 – CH 	+      CH - CH2 –(- CH –CH2 - )n - In

│	             │	  │	                 │

G	           G	  G	               G

In –( CH2 - CH - ) n- CH2 – CH – CH - CH2 –(- CH –CH2 - )n - In

│	   │	    │	                    │

G	  G	    G	                 G

Poly vinyl  Polymer.

- What are poly amide fibres ? Give an example each for a  synthetic and natural poly amide fibres.

Polymers possessing amide linkages . Ex. Nylo-6,6, is a synthetic

polyamide fibre.

Wool is an example for a natural polyamide fibre.

5.   Give reason. Molecular mass of polymers is always expressed in average.

A polymer contains chains of repeated   monomeric units  varying

lengths.

6.  On what factor does the growth of polymeric chain depend upon?

Availability of monomers in the reaction mixture.

7.  On what factors does the properties of  polymers depend upon?

Molecular mass, size and structure.

8.  Thermosetting polymers are infusible . Why ?

Due to presence of intensive cross linking.

9.  Give formula for a catalyst used in  synthesis of HDP

(C2H5)3Al and TiCl4

10. Compare and contrast  between LDP and HDP

LDP                                                 HDP

1. has highly branched structure        1. has linear molecules.

2. chemically inert and tough              2. chemically inertand tough

3. flexible                                               3.hard

4. poor conductor of electricity

SECTION E (EXERCISE QUESTIONS)

1.Explain the term polymer and momnomer.

Polymer: Macrosized molecules of high molecular mass formed by

polymerization reaction and in which very large number of repeating

structural   units are joined together by covalent bonds.

Monomer: The small molecules that combine with each other to form a

macrosized molecule called polymer .

2.What are natural and synthetic polymers? Give two examples of each type.

The polymers which are naturally found in plants and animals are called natural polymers. Ex. Proteins, Cellulose.

The man made  polymers  or the polymers which are synthesized by polymerizing simple compounds .

Ex. Nylon – 6,6., Buna – S

3.Distinguish between the terms homopolymers and copolymers and give an

example

of each.

4.How do you explain the functionality of a monomer?Define the term

polymerization.

Unsaturated compounds i.e. compounds containing double or triple bonds act as monomers because of their high reactivity towards addition reaction. In presence of a catalyst they under go repeated addition.

Monomers containing bi- functional or tri- functional groups undergo condensation  reaction to form polymers with the elimination of some simple molecules.

5.Define the term polymerization.

(Refer above )

6.Is (NH-CHR-CO)n a homopolymer or a copolymer? If so why?

A homopolymer because repeating monomeric unit is from a single monomer.

i.e  H2N – CHR -COOH

7.In which classes, the polymer are classified on the basis of molecular

forces?

Classes of polymers are

(i) Elastomers  (ii) Fibres  (iii) Thermoplastic polymers  (iv) Thermosetting

polymers.

8.How can you differentiate between addititon and condensation

polymerization?

9.Explain the term co-polymerisation and give two examples.

The process of formation of a polymer either by chain growth polymerization   or step growth polymerization of two or more  different kinds of monomers is called co-polymerisation.

Ex. Buna – S , Nylon – 6,6.

10.Write the free radical mechanism for the polymerisation of ethene.

(Refer above)

11.Define thermoplastics and thermosetting polymers with two examples of

each.

Thermoplastics: Linear or slightly branched long chain molecules capable of repeatedly softening on heating  and hardening on cooling .

Ex. Polythene, polystyrene

Thermosetting polymers: Cross linked or heavily branched molecules which on heating undergo extensive cross linking in moulds and again become infusible.

Ex. Bakelite, urea – formaldehyde.

12.Write the monomers used for getting the following polymers  (i) polyvinyl

chloride

(ii) Teflon (iii) Bakelite

(i)Poly vinyl chloride: Vinyl chloride (chloroethene)

(ii) Teflon: Tetrafluoroethene

13.Write the name and structure of one of the common initiators used in free

radical addition polymerization.

Benzoyl peroxide

O                             O

║     . .        . .          ║

C6H5 – C  - O ──   O  -     C – C6H5

. .      . .

14.How does the presence of double bonds in rubber molecules influence

their structure and reactivity?

Due to presence of double bond it may have either cis or trans  orientation.But in natural rubber all double bonds have cis stereochemistry. Natural rubber is cis- poly isoprene.

Cis –poly isoprene chains held together by van der waal’s forces and has a coiled structure. Chain can be stretched like a spring and exhibits elastic properties.It becomes soft at high temperature and becomes brittle at lower temperature and show high water absorption capacity and also non-resistant to oxidizing agents.

15.Discuss the main purpose of vulcanization of rubber.

Natural rubber because of its structure becomes soft at a temperature above 335K  and becomes brittle  below 283K, show high water absorption capacity,soluble in non- polar solvents and non – resistant to oxidizing agents.Hence it is  not so usefull. To overcome these properties vulcanization is done.

When vulcanization is done rubber gets stiffened  due to formation of S cross links.

16.What are the monomeric repeating units of Nylon – 6 and  Nylon – 6,6?

(refer above )

17.Write the names and structures of the monomers of the following

polymers:

  - Buns –S (ii) Buna  - N (iii) Dacron  (iv) Neoprene

- Buna  - N monomers :1,3 – Buitadiene and acrylonitrile (ethene

nitrile)

CN

│

CH2 = CH – CH = CH2    and  CH2 = CH

1,3 –Butadiene.

18.Identify the monomer in the following polymeric structures.

(i)

O                O

║                  ║

Monomers are     H –O – C – (CH2)8- C –O – H  and   H2N – (CH2)6 – NH2

Adipic acid (1,10- Decane dioic acid )     Hexamethylene diamine.

(Hexane -1,6-diamine)

(ii)

Monomers are

19.How is decron obtained form ethylene glycol and terepthalic acid?

(Refer above)

20.What is a biodegradable polymer?Give an example of a biodegradable

aliphatic polyester.

A biodegradable aliphatic poly ester is Poly β-hydroxybutyrate –co- β –hydroxy valerate (PHBV)

PREPARED BY :

NAYAK UDAY D.

P.G.T.IN CHEMISTRY,J.N.V.CHIKMAGALURE,MOB.NO;9449620408

# Text boxes

O

O

C    ( CH2)8      C      NH      (CH2)6 –NH              n

n

HN

NH-CH2-

NH

N

N

N

H                    H   O                   O

║

N – (CH2)6 – N – C -  (CH2)4 -  C

n

o

║

CH2

CH2

C = O        533- 543 K

H2C

CH2

H2C

H

│

N

n

NH2

NH2

O

N

N

N

H2N

O

C    ( CH2)8      C      NH      (CH2)6 –NH              n

+

HCHO

H+

CH2

--CH2

CH2

CH2--- --

H2N

NH2

NH2

N

N

N

+

HCHO

formaldehyde

H2N

H2N

NHCH2OH

N

N

N

N

N

N

and    HCHO

N